## Slide 1
Four wave mixing in submicron waveguides

## Slide 2: Basis
Refractive index is dependent on the light intensity
nonlinear refractive index
Nonlinear phase shift is generated during propagation
Propagation constant is also dependent on light intensity (power)
nonlinear coefficient
idler
signal
pump
waveguide
Pump
Signal
Idler
Energy from the pump is transferred to the signal and idler
Material with 3rd order nonlinearity – χ(3)
Notes: What is four wave mixing? The simplest case of FWM is simple generation of third wave when we input two different waves into nonlinear medium. Depending on wavelength difference between two entering waves third wave will be generated on the other side of the pump wave, symmetrically with respect of the signal wave. How this happened? Basically energy from strong pump is transferred to the signal that would be amplified and a new idler wave that will be generated simultaneously. In this case two pump photons are destroyed and their energy appears in two new photons.
What is the physics below? Refractive index of the medium is dependent on the light intensity. This means that optical wave passing through the medium is changing conditions of own propagation. Since the refractive index is related to propagation constant, prop.const. is also intensity dependent. This can introduce nonlinear phase shift dependent on input power during light propagation.

## Slide 3: Applications
Wavelength conversion
Nonlinear medium
CW Pump
Signal Channel
Optical filter
Idler
Possible to transfer data from signal to the idler wave at the new wavelength
Optical sampling
J. V. Erps et al., J. Lightwave Technol. 21 (2010) 209-15.
Sampling of high speed signals beyond the limits of electronics
Short samplings pulses act as the pump  Idler pulse width comparable to pump pulses

## Slide 4: Different nonlinear media
Waveguide
Advantages
Problems
SiO2 highly nonlinear fiber
Extended length
n2 ~ 10-20 m2/W
Stimulated Brillouin scattering
Low losses
Silicon waveguides
n2 ~ 10-18 m2/W
Strong confinement
Length is shortened
Two photon absorption
Increased losses
III-V waveguides
Three photon absorption
n2 ~ 10-17 m2/W
No two photon absorption
Photonic crystals waveguides
Fabrication
Separate engineering of D and γ
Slow light regime

## Slide 5: Outline
Motivation
Phase – matching
Characterization needs
  Dispersion characterization
  Nonlinear characterization
  Conversion bandwidth

## Slide 6: Phase matching
Conversion efficiency:
Depends on phase matching parameter:
Linear phase mismatch:
Therefore essential to be able to measure dispersion over a broad bandwidth as well the nonlinear coefficient 
idler
signal
pump
CE
Notes: Parametric interactions are strongest when the process is phasematched.

## Slide 7: Dispersion characterisation
Low coherence interferometer being implemented
Free space Mach-Zehnder interferometer structure
SOA used as broadband source
Good method to characterise dispersion over broad bandwidth
As required for phase matching evaluation

## Slide 8: Nonlinear coefficient characterisation
waveguide under test
OSA
CW
CW
Att.
EDFA
PWM
A. Boskovic et al., Opt. Lett. 21 (1996) 1966-8.
Pin is the sum of the power of the 2 lasers at the waveguide input
with
If the waveguide dispersion can be neglected ( small wavelength separation between lasers)
Measure I0 , I1 , versus Pin
Retrieve γ

## Slide 9: Nonlinear coefficient measurement
Facet loss [dB] | 7.82 (TE) | 7.76 (TM)
Propagation loss [dB/cm] | 2.66 | 1.95
γ [1/Wm] | 151.56 | 145.91
h = 340 nm
w = 500 nm
substrate
Si
SiO2
h
w
Good agreement with theoretical calculation
Output of the chip
Calculation:
Notes: Discuss about linear fit. It is not perfectly linear because fwm efficiency was not that big?

## Slide 10: Conversion efficiency
Different models used by groups working in the field
N. Shibata et al., J. Quantum Electron. 23 (1987) 1205-10.
No nonlinear phase matching
No pump depletion
M.E. Heidari et al., Opt. Express 17 (2009) 18340-53.
Modified pump power
No pump depletion
No loss
No pump depletion
R.H. Stolen et al., J. Quantum Electron.18 (1982) 1062-71
Losses taken into account
No pump depletion
K. Wang et al., Opt. Lett. 37 (2012) 1331-3.
Notes: It is important to know what is CE bandwidth if we want to demonstrate FWM in nanowires. In order to predict conversion efficiency different models are used by groups working in the field.
Besides those analytical models there is also numerical model, which is exact, but than we are loosing sense of physics. It is also important to mention that model developed by Shibata is in very good agreement with numerical calculations.

## Slide 11: Conversion efficiency bandwidth
Example:
Exact solution obtained using numerical method
Bandwidth for Stolen Leff is overestimated
Maximum conversion efficiency for Stolen model is overestimated – model does not include loses
Bandwidth for Shibata model and Modified Stolen model are very close
substrate
Si
SiO2
h
w
h = 205 nm
w = 900 nm

## Slide 12: Conclusions
Conversion efficiency and the FWM bandwidth can be further increased in waveguides.
Phase matched nonlinear processes like FWM benefit from the use of engineered waveguides through dispersion engineering, which ensures phase matching over a large bandwidth.
Using FWM in new materials photonic waveguides should continue to provide unique nonlinear optical functionality at even lower power levels.
Thank you 